# Contact Information

| name: | e-mail: |
| --- | --- |
| address: | phone: |

# Project

Powder coat Porsche 928 Parts: intake (with separate left and right end plates), two cam covers, water bridge, and thermostat elbow.

# Powder Selection

| base coat: | top coat: |
| --- | --- |

# Additional Items Supplied

# Part: Intake

## General Information:

- Material: aluminum/magnesium alloy

- Coat this part promptly after baking; it oxidizes quickly!

## Cleaning

- Strip all interior and exterior surfaces using chemical strippers and media blasting.

- Bake until you are sure all oils and contaminants have been outgassed.

## Masking

Mask, plug, and cap using the following annotated photos as a guide.

Top:

Bottom:

Right side (left side is just mirror image of right side):

# Part: Intake End Plates

## General Information:

- Material: aluminum/magnesium alloy

- Coat this part promptly after baking; it oxidizes quickly!

## Cleaning

- Strip all interior and exterior surfaces using chemical strippers and media blasting.

- Bake until you are sure all oils and contaminants have been outgassed.

## Masking

Mask and plug using the following annotated photos as a guide.

Front:

Back:

# Part: Cam Covers (Two Identical Units)

## General Information:

- Material: aluminum/magnesium alloy

- Coat this part promptly after baking; it oxidizes quickly!

## Cleaning

- Strip all interior and exterior surfaces using chemical strippers and media blasting.

- Bake until you are sure all oils and contaminants have been outgassed.

## Masking

Mask and plug using the following annotated photos as a guide.

| Front: | Back: |
| --- | --- |

# Part: Water Bridge

## General Information:

- Material: aluminum

## Cleaning

- Strip all interior (as much as possible) and exterior surfaces using chemical strippers and media blasting.

- Bake until you are sure all oils and contaminants have been outgassed.

## Masking

Mask and plug using the following annotated photos as a guide.

Top:

Bottom:

Front:

# Part: Thermostat Elbow

## General Information:

- Material: aluminum

## Cleaning

- Strip all interior (as much as possible) and exterior surfaces using chemical strippers and media blasting.

- Bake until you are sure all oils and contaminants have been outgassed.

## Masking

Mask and plug using the following annotated photo as a guide.

# Text boxes

date: